# 1. Product Description

| Product description | : | SUPER GLUE is a quick setting adhesive |
| --- | --- | --- |
| Use of the substance/mixture | : | adhesives |
| Recommended use | : | Industrial use Professional uses Consumer use |

2. Characteristics

| Characteristics | : | Very high bond strength after a few seconds |
| --- | --- | --- |

3. Application

Using for adhering metals, leather, ceramic, porcelain, china, pottery, rubber, most plastics, hard and soft woods, jewellery, fingernail Not for using with glass, rear view mirrors, Teflon, polyethylene, polypropylene, certain silicone rubber types or surfaces which are exposed to great shock or continuous immersion in water

# 4. Application Instructions

Application temperature is between -15 °C and +40°C Make sure the surface to be applied is dry and clean for best results Protect clothing and work surfaces (metal foil works well) Use in a well-ventilated area Carefully follow tube opening directions on package Unscrew cap while keeping tube pointed away from face Apply to one surface, using 1 drop per square inch of surface Assemble parts and hold together with pressure for 15 seconds or until set Wipe top of nozzle if adhesive has accumulated before recapping tube securely after

# 5. Technical Specifications (@ 23 °C 50% RH)

| Appearance | : | Liquid |
| --- | --- | --- |
| Colour | : | Clear,Transparent |
| Final Colour | : | Clear |
| Odour | : | Characteristic |
| Set Time | : | 5-10 second |
| Full Strength | : | 24 hours |
| Application Temperature | : | -15 - 40 °C |

# 6. Packaging

| Bottle 20 g | Package 10x50=500 |
| --- | --- |
| Bottle 50 g | Package 4x40=160 |

# 7. Shelf Life and Storage

| Storage conditions | : | Store locked up. Store in a well-ventilated place. Keep container tightly closed. Keep cool. |
| --- | --- | --- |
| Storage temperature | : | -15 - 40 °C |

| Bottle 20 g | 12 months (after production date if stored at room temperature) |
| --- | --- |
| Bottle 50 g | 12 months (after production date if stored at room temperature) |

# 8. Health and Safety

| Adverse physicochemical, human health and environmental effects | : | May cause respiratory irritation,Causes skin irritation,Causes serious eye irritation. |
| --- | --- | --- |
| First-aid measures general | : | Call a poison center or a doctor if you feel unwell. |
| First-aid measures after inhalation | : | Remove person to fresh air and keep comfortable for breathing. Call a poison center or a doctor if you feel unwell. |
| First-aid measures after skin contact | : | Wash skin with plenty of water. Take off contaminated clothing. If skin irritation occurs: Get medical advice/attention. |
| First-aid measures after eye contact | : | Rinse cautiously with water for several minutes. Remove contact lenses, if present and easy to do. Continue rinsing. If eye irritation persists: Get medical advice/attention. |
| First-aid measures after ingestion | : | Call a poison center or a doctor if you feel unwell. |
| Symptoms/effects after inhalation | : | May cause respiratory irritation. |
| Symptoms/effects after skin contact | : | Irritation. |
| Symptoms/effects after eye contact | : | Eye irritation. |
| Other medical advice or treatment | : | Treat symptomatically. |
| Hand protection | : | Protective gloves |
| Eye protection | : | Safety glasses |
| Skin and body protection | : | Wear suitable protective clothing |
| Respiratory protection | : | In case of insufficient ventilation, wear suitable respiratory equipment |

# 9. Remarks

| Remarks | : | For further information, please refer to the Safety Data Sheet |
| --- | --- | --- |

No additional information available

# 10. Standards and Certificates

No information available

Technical Data Sheet

This information is based on our current knowledge and is intended to describe the product for the purposes of health, safety and environmental requirements only. It should not therefore be construed as guaranteeing any specific property of the product